| APPLIED RESEARCH |
| --- |
| Development of high efficiency long wavelength infrared radiators for medical application in area of human physiotherapy and sterilizing treatment of rooms or medical equipment |
| Description The main task of this development is choice material, investigate its properties and create technology for production of high efficiency infrared sources of thermal energy. The idea to use layered gradient ceramics was developed by V. Petrovsky and gives possibility to solve next problems: Increase the wavelength range up to 7 - 12 (m at the same or higher surface temperature.. Decrease the power consumption of one heater up to 25-30%. Such distribution of energy sufficiently increased physiotherapy efficiency and reduce power consumption above 450W per physiotherapy chamber. Create essentially new system for sterilizing treatment equipment: the two heaters with sizes 100 x 8 x 8mm3 can radiate 825 Watt for heating the air blast (under pressure 8 atm. the speed is about 20 km/h at the temperature 300°C.) This heated air blast can obliterate all bacteria and microbes on any surface during parts of second. Innovative Aspect and Main Advantages Decrease the power consumption at some thermal efficiency. Follow on the concept of layered composite there are offered the three type of IR radiators: (i) low temperature IR radiator based on layered structure of composite based on heat source from flexible ribbon heater (Fig.1) and IR radiated surface based on glass ceramic (temperature range before 150°C) (fig.2); (ii) middle temperature IR radiator based on heat source from flexible ribbon and IR radiated surface based on heater silicon nitride (temperature range 300-550°C); (iii) high temperature all ceramic IR radiator (temperature range 500-1100°C) for utilization at condition of intense heat-exchange (Fig.3). Fig.1. Flexible ribbon as heat sources. |  | Fig.2. Low temperature IR radiator as electrical heater for industrial and living rooms (The efficiency is 2 times more as compared with oil heater) Fig.3. All ceramic IR radiator and their utilization as heater to extra high heat emission in new system for sterilizing treatment equipment Areas of Application Energy sawing electrical heating of industrials and living rooms; medical application in area of human physiotherapy; system for sterilizing treatment equipment of rooms or medical equipment. Stage of Development (i) Low temperature IR radiator for industrial and living rooms – commercialized; (ii) Middle temperature IR radiator for of human physiotherapy and (iii) high temperature all ceramic IR radiator for sterilizing treatment - prototype available for testing; Contact Details Contact person: Professor Vitaly Petrovsky Company name: Institute for Problems of Materials Science Ukrainian Academy of Sciences Street: 3, Krzhyzhanovsky Str. Country: Ukraine; Postcode: 03680; City: Kiev Phone: +38044 424 1531; Fax: +380 44 424 5452 E-Mail: gradient@zeos.net Web: www.uagradient.net |