| MEDICAL INSTRUMENTATION AND BIOMEDICAL TECHNOLOGIES |
| --- |
| NEW MAGNESIUM-BASED ALLOY FOR MEDICINE |
| Description In NSC KIPT new magnesium-based alloy have developed, witch distinguished by high mechanical characteristics (strength and plasticity) and by the increased corrosion stability in biosystem of a human body. On series parameters the developed material surpasses alloy WE43 biodegradable in vivo. The offered alloy with ultra fine-grained (UFG) structure (medial grain size < 1 micron) has YS ( 200 MPa, UTS ( 300 MPa, ( ( 30 %, and on a corrosion resistance can compete to alloy WE43. The production technology of material forming in a superplastic condition can be used at temperature 300 0С and small strain rates for production of tubes and other products from a developed alloy. Thin-walled tubes from an alloy, fit for a cutting-out from them coronary stents and a wire by a diameter of 0.3 mm are received. Dependence of mechanical characteristics of a material on processing conditions by pressure and a high-heat treatment is explored. Innovative Aspect and Main Advantages The offered alloy in UFG a condition on mechanical characteristics surpasses production released alloy WE43. Plasticity of a new alloy at ambient temperature attains 30 %. The alloy has well formability, which allows forming of it the fine wire, thin-walled tubes and products of composite forms. Due to the increased corrosion stability the alloy can be used for manufacture of biocompatible products of medical purpose. Areas of Application The offered magnesium-based alloy can be used for manufacture: Coronary and peripheral stents for an angioplasty. Connecting products for bone surgery. Parts of biosoluble devices for a radioactive irradiation in oncology. |  | Fig.1. Grain structure of magnesium- based alloy in UFG condition. Stage of Development Thin-walled tubes and wire from the developed alloy are manufactured. Properties of tubes and wire are explored. The European patent application is fed. Search of cooperation for the further development and use. Contact Details Ukraine, Kharkov 61108, Akademichna str, ap. 1 National Science Center “Kharkov Institute of Physics and Technology” Papirov Igor Isakovich, Тел. +38 (057) 335-60-27 E-mail: papirov@kipt.kharkov.ua STCU Senior Specialist: Nataliya Mykhaylovska [nataliya.mykhaylovska@stcu.int] STCU Technology reference: TPFe 157_01 |

# Text boxes

TPFe 204_01

5 mkm